## Slide 1
Polarization, geometry dependence, sum rules and tensor formulation in XAS and RIXS
Michelangelo Tagliavini
European Xfel,
michelangelo.tagliavini@xfel.eu

## Slide 2: Dichroism
Linear
Circular
Images: H. Elnaggar
y
Notes: I think most of us are familiar with dichroism in the optical regime from our daily lives. For example from polarized glasses and how it avoids glare.
Glare tends to happen when lightwaves strike a flat surface, causing the light to reflect, or bounce off the surface, in a horizontal manner (brewster law). This causes the light to be intense, which can hurt the eyes and make it more difficult to see.
The filters on polarized lenses absorbs LH light and hence stops the glare.

## Slide 3: Dichroism
Dichroism:
Difference of the propagation of light measured with
two orthogonal polarization
states of the incoming light
Avoid glare (LH light)
Slide: H. Elnaggar
Notes: I think most of us are familiar with dichroism in the optical regime from our daily lives. For example from polarized glasses and how it avoids glare.
Glare tends to happen when lightwaves strike a flat surface, causing the light to reflect, or bounce off the surface, in a horizontal manner (brewster law). This causes the light to be intense, which can hurt the eyes and make it more difficult to see.
The filters on polarized lenses absorbs LH light and hence stops the glare.

## Slide 4: Introduction to X-ray dichroism
Linear Dichroism (LD):
Difference measured with LH / LV
Circular Dichroism (CD):
Difference measured with CR / CL
Natural Dichroism (ND):
Difference in magnetic system
Measurement:
Origin:
Magnetic Dichroism (MD):
Difference in structurally distorted system
Magneto-chiral Dichroism (MχD):
Difference in a magnetic + chiral system
And more …
Slide: H. Elnaggar
Notes: So similar to the optical regime, dichrosim effect is also present in the x-ray regime.
And there are many different types of dichroism and classifications.
For example, it can be classified according to the measurement. So in this case we can say that it is linear dichroism when it is measured with linear light.

## Slide 5: Why do we need X-ray dichroism?
The measurement of dichroism is often challenging…
Control polarization, orientation of sample, single crystals required, several measurements …
but provides access to properties that can be lost in the average measurements!
How can we understand X-ray polarization dependence and dichroism?
X-ray Linear (XLD) and Magnetic circular Dichroism (XMCD)
Can we predict all X-ray dichroism effects?
Extensions to RIXS.
What we will discuss:

## Slide 6: Core to Valence transition Operator
https://en.wikipedia.org/wiki/Rubber_duck

## Slide 7: Excitations in XAS
Final state
Initial state
Transition operator
Fermi golden rule!
Slide: H. Elnaggar

## Slide 8: Electric light-matter excitations
Polarization vector
Position vector
Wave vector
Taylor expansion:
Dipole
Quadrupole
Slide: H. Elnaggar

## Slide 9: Dipole transition operator
Expression in terms of l=1 spherical harmonics (p orbitals):
Dipole:
Examples: TM L2,3 , Ln, An M4,5 edges
Defined wrt to the crystal axes
Slide: H. Elnaggar

## Slide 10: Quadrupole transition operator
Quadrupole:
Expression in l=2 spherical harmonics (d orbitals):
Examples: transition operator used for TM K pre-edges .
Slide: H. Elnaggar

## Slide 11: Xray Linear Dichroism (XLD)
https://en.wikipedia.org/wiki/Rubber_duck

## Slide 12: X-ray Linear Dichroism in Oh Cu2+
eg:(dx2- y2, dz2)
t2g:(dxy, dzy, dzx)
d9
Slide: H. Elnaggar

## Slide 13: X-ray Linear Dichroism in Oh Cu2+
Dipole
(think p orbitals)
<f¦ | T | ¦i>
y
z
x
z
x
y
y
z
x
z
x
y
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Slide: H. Elnaggar

## Slide 14: X-ray Linear Dichroism in Oh Cu2+
<f¦ | T | ¦i>
y
z
x
z
x
y
y
z
x
z
x
y
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Dipole
(think p orbitals)
Slide: H. Elnaggar

## Slide 15: X-ray Linear Dichroism in Oh Cu2+
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Dipole
(think p orbitals)
<f¦ | T | ¦i>
y
z
x
z
x
y
y
z
x
Slide: H. Elnaggar

## Slide 16: X-ray Linear Dichroism in Oh symmetry
Quanty Calculation of L2,3 XAS of Oh Cu2+
Experimental results of K-edge XAS of Oh Cr3+ in MgAl2O4
Dipole: p -> d
Dipole: s -> p
Juhin et. al., Phys. Rev. B 78, 195103, 2008
Dipole transition in Oh symmetry are isotropic !
Slide: H. Elnaggar

## Slide 17: Dipole XLD in reduced symmetry
a1g:(dz2)
b2g:(dxy)
d9
eg:( dzy, dzx)
b1g:(dx2- y2 )
Elongated Oh
Slide: H. Elnaggar

## Slide 18: X-ray Linear Dichroism in D4h Cu2+
Dipole
(think p orbitals)
<f¦ | T | ¦i>
z
x
y
z
x
y
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Slide: H. Elnaggar

## Slide 19: X-ray Linear Dichroism in D4h Cu2+
<f¦ | T | ¦i>
z
x
y
z
x
y
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Dipole
(think p orbitals)
Slide: H. Elnaggar

## Slide 20: X-ray Linear Dichroism in D4h Cu2+
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Dipole
(think p orbitals)
<f¦ | T | ¦i>
z
x
y
Slide: H. Elnaggar

## Slide 21: X-ray Linear Dichroism in D4h symmetry
Quanty Calculation of L2,3 XAS of D4h Cu2+
Experimental results of L2,3 XAS of D4h Fe2+
Dipole transition in lower symmetries give rise to X-ray Linear Dichroism
XLD tells us which holes are these
Schofield et. al., Miner. B 62, 65, 1998
Slide: H. Elnaggar

## Slide 22: Xray Magnetic Circular Dichroism (XMCD)
https://en.wikipedia.org/wiki/Rubber_duck

## Slide 23: X-ray Magnetic Circular Dichroism (XMCD)
Thole et. al., Phys. Rev. lett. (1992). 68
B
B
For ferro/ferri-magnetic materials
At L3,2 edges:
Valence band has a spin-imbalance due to the magnetic ordering
Right- and left-circularly polarized photons carry opposite momentum (+1, -1)
Angular momentum of the photon interacts with the spin of the electron by means of the SOC
Slide: H. Elnaggar
Notes: Angular momentum of the photon interacts with the spin of the electron by means of the SOC (Fano effect).
◮ Right- and left-circularly polarized photons carry opposite momentum ⇒ there is a spin imbalance in the photocurrent produced by the right- and left-circularly polarized x-rays.
2. Valence band acts as a spin detector for the (spin-imbalanced) photocurrent.

## Slide 24: XMCD in CoFe2O4
Sum rules:
Relate dichroism to the average ground state magnetic moment
Experimental results of Fe L2,3 XMCD
Slide: H. Elnaggar

## Slide 25: The XAS conductivity tensor
https://en.wikipedia.org/wiki/Rubber_duck

## Slide 26: General expression of the XAS

## Slide 27: General expression of the XAS
Off-diagonal: ->
y polarized light is changed by the system to an x polarized
Low symmetry system or magnetic system
Rank 2, dim. 3 tensor:
rXGrX | rXGry | rXGrz
rYGrX | ryGry | ryGrz
rzGrX | rzGry | rzGrz
Slide: H. Elnaggar

## Slide 28: Application of group theory
Rank 2, dim. 3 tensor:
rXGrX | rXGry | rXGrz
rYGrX | ryGry | ryGrz
rzGrX | rzGry | rzGrz
The tensor reflects the local symmetry of the probed atomic position. Group theory gives compact rules to predict its form.
For dipole interactions, each photon couples an angular momentum l=1 to the sample.
If the system is time reversal symmetric, the XAS tensor is symmetric!

## Slide 29: X-ray Linear Dichroism
Oh
Symmetry | x | y | z
Oh | t1g | t1g | t1g
εx
Images: M. W. Haverkort

## Slide 30: X-ray Linear Dichroism
Oh
Symmetry | x | y | z
Oh | t1g |  | 
εz
Images: M. W. Haverkort

## Slide 31: X-ray Linear Dichroism
Oh
Symmetry | x | y | z
Oh | t1g |  | 
ε= x+y
Images: M. W. Haverkort

## Slide 32: X-ray Linear Dichroism
Images: M. W. Haverkort
D4h
Symmetry | x | y | z
D4h | eg |  | a2g

## Slide 33: X-ray Linear Dichroism
Images: A. Juhin
Monoclinic
Symmetry | x | y | z
c2 | b | b | a

## Slide 34: X-ray Magnetic Circular Dichroism
Magnetism breaks time reversal symmetry of <riGrj>.
This results in the asymmetry of the off-diagonal elements
Slide: H. Elnaggar

## Slide 35: X-ray Magnetic Circular Dichroism
Images: H. Elnaggar

## Slide 36: X-ray Magnetic Circular Dichroism
Images: H. Elnaggar

## Slide 37: Rotations
e.g, rotate Oh
Images: A. Juhin

## Slide 38
Solutions and Powders

## Slide 39: Sum Rules for XMCD
XMCD ∼ avg orbital magnetic moment
Isotropic ∼ number of holes
XMCD ∼ avg spin magnetic moment
Thole et. al., Phys. Rev. lett, 68, 1992
Slide: H. Elnaggar
Notes: One can deduce ground state proper

## Slide 40: Sum Rules for XMCD
XMCD ∼ avg spin magnetic moment
Thole et. al., Phys. Rev. lett, 68, 1992
I1/2(L2)
I3/2(L3)
l is the angular momentum of the valence shell, here l=2.
Images: H. Elnaggar
Notes: One can deduce ground state proper

## Slide 41: However …
Issues to consider:
Background removal
(edge position, mixing of edges, detection mode “FY?”)
Can be calculated by Quanty!
Magnetic dipole term
Slide: H. Elnaggar
Notes: Tz : provides a measure of the anisotropy of the field of the spins when the atomic cloud is distorted, either by the spin-orbit interaction or by crystal-field effects [7].

## Slide 42
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Nine linear independent measurements to construct the full tensor
Slide: H. Elnaggar
Measuring the Full XAS tensor
Here: Magnetite (Fe3O4)

## Slide 43
Dichroism is originated by local symmetry breaking of the system. Lower Symmetry (e.g. Oh to D4h)
    → Ground state degeneracy splits.
    → Final state energy also splits.
All dichroism effects can be represented in a compact way by the XAS conductivity tensor.
The XAS response function is time reversal symmetric. → asymmetry of the tensor is a signature of a magnetic system.
Sum rules can be used to extract occupation and orbital expectation values for the Ground state.
XAS- concluding Remarks

## Slide 44: Repeat, but for RIXS
https://en.wikipedia.org/wiki/Rubber_duck

## Slide 45
RIXS | Tensor formulation
Tagliavini, Wenzel, Haverkort, PRB 113, 195122 (2026)

## Slide 46
Polarization Basis in Cubic Harmonics
Mathematica Script in the tutorials!
←Rotors. l=1, but even

## Slide 47
Polarization Basis in Cubic Harmonics
Mathematica Script in the tutorials!

## Slide 48
Spectrum in Oh

## Slide 49
Spectrum in Oh

## Slide 50
Point Group Theory → # of independent spectra
Here: q independent processes

## Slide 51
Compute RIXS spectrum without polarization Filter
Fumagalli et. al. PHYSICAL REVIEW B 99, 134517 (2019)

## Slide 52
Powder Averaging | Same as for XAS
Here: q independent processes

## Slide 53
Powder Averaging
!New! Quanty function to compute powder spectra!
→ In order to get access to the third linear independent component, we need to have to measure in circular polarization for both ingoing and outgoing photons!

## Slide 54
Dichroism Options in RIXS – “Linear Dichroism”
B. T, Chiogo, PHYSICAL REVIEW B 106, 075141 (2022)
Fixed scattering Geometry, change linear and vertical ingoing polarization→ Change between composition of angular momentum transfer.
2θ=90°

## Slide 55
Dichroism Options in RIXS – Sample rotations
M. Moretti Sala et. al NewJ.Phys. 13 043026 (2011)
δ=+45°
2
-i2
2
i2
2
2
*1/16
LCO, 2θ=90°

## Slide 56
Dichroism Options in RIXS – Sample rotations
M. Moretti Sala et. al NewJ.Phys. 13 043026 (2011)
δ=0°
4
-i2
3
i2
1
2
2
2
*1/32
2
LCO, 2θ=90°

## Slide 57
Dichroism Options in RIXS – Sample rotations
M. Moretti Sala et. al NewJ.Phys. 13 043026 (2011)
δ=-45°
2
2
2
2
*1/16
Mathematica Script in the tutorials!
LCO, 2θ=90°

## Slide 58
kin=z
Dichroism Options in RIXS – RIXS-CD
-i
+i
+i
-i
1
1
-1
-1
I(left,z)-I(right,z)
εout= z
Circular right
Circular left
Bext//z
RIXS tensor not invariant under time inversion→There is no symmetry of the tensor which are broken under magnetic ordering. → Cannot say if structural or magnetic driven
Furo et. al. PHYSICAL REVIEW B 112, 214429 (2025)

## Slide 59
kin=z
RIXS-CD – Chiral Magnons
εout= z
Circular right
Circular left
Bext//z
RIXS not invariant under time inversion→There is no symmetry of the tensor which are broken under magnetic ordering. → Cannot say if structural or magnetic driven
Jost et. al. arXiv:2501.17380 (2025)
“Altermagnons”?

## Slide 60
Selection rules for the RIXS final state: 3d9 D4h example
Due to the intermediate state spin-orbit interactions, double groups should be considered to get the exact selection rules. However, for shallow core holes or light elements, the main excitations are given by the single group selecton rules.

## Slide 61
The RIXS conductivity tensor is also sensitive to symmetry breaking.
  # Linear independent contributions depends on symmetry.
  Interpretation of RIXS tensor not straight forward.
Different way to control dichroism:
  Change polarization and scattering angle: vary χ(0), χ(1) and χ(2) spectral contribution.
  Rotate the sample: vary the dmixture of the sub-contributions for each l=1 and l=2.
Learned how to:
  Spectrum for no outgoing polarization analysis.
  Spectrum for Powders.
Extension to dispersive excitations and Quadrupole/Magnetic interactions possible.
RIXS- concluding Remarks

## Slide 62: Appendix
https://en.wikipedia.org/wiki/Rubber_duck

## Slide 63
Spectrum in Oh

## Slide 64
Dichroism Options in RIXS – “RIXS-CD” in coupled spherical harmonics basis
i2√3
-i2√3
-3+√3
6
-3+√3
6
I(left)-I(right)
kin=z
εout= z
Circular right
Bext//z

## Slide 65
Bragg spectrometer as a polarization filter

## Slide 66
Magnetite: [Fe3+]Td [Fe2+ , Fe3+]OhO4
Magnetite: Fe L3,2-edge XAS
Ferrimagnetic system:
  We expect to measure XMCD and that the tensor has off-diagonal elements
The Fe2+ Oh are distorted to D3d:
  We expect to measure XLD and that the tensor has different components in various directions
Slide: H. Elnaggar

## Slide 67
To get all elements:
9 independent measurements
Linear polarization (diagonals + symmetric off diagonals)
Circular polarization (asymmetric off diagonals)
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Magnetite: Fe L3,2-edge XAS
Imaginary: measured
Real: transformation
Slide: H. Elnaggar

## Slide 68
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Building the tensor
Slide: H. Elnaggar

## Slide 69
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
XMLD in dipole cubic
symmetry due to magnetism!
Analyzing the tensor: Diagonal XMLD
Slide: H. Elnaggar

## Slide 70
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
XMCD in cubic symmetry
Analyzing the tensor: XMCD
Slide: H. Elnaggar

## Slide 71
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
XMLD signature of small non-cubic distortion leading to mixing of x-z direction
Analyzing the tensor: small distortion
Slide: H. Elnaggar