## Slide 1
Atomic multiplet theory of XAS
Crystal field theory of XAS
Screening in XAS and XPS spectral shapes
Charge transfer theory of XPS
XAS, XMCD and XPS spectral shapes

## Slide 2
atom
solid
atomic
multiplet
theory
empty
density
of states
XAS: spectral shapes in
atoms and solids
spin-orbit coupling
Intra-atomic
electron-electron interactions
Inter-atomic
electron-electron interactions

## Slide 3
atomic
multiplet
theory
empty
density
of states
XAS: spectral shapes in
atoms and solids
spin-orbit coupling
Intra-atomic
electron-electron interactions
Inter-atomic
electron-electron interactions (only symmetry
as effective field)
crystal field
multiplet
theory

## Slide 4
2p XAS of TiO2
2p XAS of Ti4+ ions
Ground state of Ti4+ is 3d0
Dipole transition 3d02p53d1
Ground state symmetry: 1S0
Final state symmetry: 2P2D gives
1P, 1D, 1F, and 3P, 3D, 3F
Atomic multiplets: 2p XAS of Ti4+

## Slide 6
3d0 XAS calculation
Atomic multiplets: 2p XAS of Ca atoms

## Slide 7
3d0 XAS calculation
Atomic multiplets: 2p XAS of Ca atoms

## Slide 8
3d0 XAS calculation
Spin-orbit = 4.0 eV
Electron-electron = 5.0 eV
Spin-orbit = 0.4 eV
Electron-electron = 9 eV
Atomic multiplets: 2p XAS of Ti4+

## Slide 9
ATOMIC MULTIPLETS 3d1
5 orbitals (each spin-up or spin-down) >> total 10 states
No electron-electron interaction: all states have the same energy
Quantum numbers: L=2 and S=½, notation as term symbol: 2S+1L= 2D

## Slide 10
ATOMIC MULTIPLETS 3d1
Spin-orbit coupling couples L and S quantum numbers to a total quantum number J
Jmax= L+S = 5/2, Jmin= |L-S|= 3/2, Integer steps of J.
Two term symbols: L=2, S=½, and J = 5/2 >> notation as term symbol: 2S+1LJ= 2D5/2
L=2, S=½, and J = 3/2 >> notation as term symbol: 2S+1LJ= 2D3/2

## Slide 11
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d1
3d1
2D
2D3/2
2D5/2
electron-electron
interaction
spin-orbit
coupling
(~50 meV)

## Slide 12
2p XAS of TiO2
2p XAS of Cu2+ ions
Ground state of Cu2+ is 3d9
Dipole transition 3d92p53d10
Ground state symmetry: 2D5/2
Final state symmetry: 2P gives
2P3/2 and 2P1/2
Atomic multiplets: 2p XAS of Cu2+

## Slide 13
Atomic Multiplet Theory
X-ray absorption from 3d9 to 2p53d10

## Slide 14
MCD
MCD
mJ=-5/2
to
mJ’=-3/2
no LS
X-MCD
X-ray absorption from 3d9 to 2p53d10

## Slide 15
Atomic Multiplet Theory
Operator symmetry in X-MCD
SO3 | Oh | D4h | C4 | 
S | A1 | A1 | z | 
P | A2 | B1 | left | 
D | E | E | right | 
F | T1 | A2 |  | 
G | T2 | B2 |  | 

## Slide 16
X-MCD
Cu2+: 3d9
X-ray MCD

## Slide 17
MCD
MCD
mJ=-5/2
to
mJ’=-3/2
no LS
X-MCD
X-ray MCD

## Slide 18
X-MCD
no LS
MCD
+ crystal field
MCD
X-ray MCD

## Slide 19
ATOMIC MULTIPLETS 3d2
5 spin-up orbitals give 4 + 3 + 2 + 1 = 10 paired 3d2 states
5 spin-down orbitals give 10 paired down-down 3d2 states
There are 5x5 = 25 up-down states
In total 10+10+25 = 45 states
Can also be calculated as 10 x 9 / 2 = 45 states
Electron-electron interaction is different for different orbital combinations
There will be a number of different states with different energies.
Analysis shows that the states are 1S, 3P, 1D, 3F and 1G

## Slide 20
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d2
3d2
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
electron-electron
Interaction
(~2 eV)
spin-orbit
coupling
(~50 meV)
    Ground state:
    Given by Hunds rules
    max S
    max L
    min J (if less than half full)

## Slide 21
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d8
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
electron-electron
Interaction
(~2 eV)
spin-orbit
coupling
(~50 meV)
    Ground state:
    Given by Hunds rules
    max S
    max L
    max J (if more than half full)

## Slide 22
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 23
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 24
Atomic multiplets
2p XAS of NiO with atomic multiplets

## Slide 25
Term Symbols of 2p2
Energies of the term symbols
Slater-Condon | Electron-electron interaction | Slater | Racah | Kanamori
F0 | Direct term | F0=F0 | A= F0 -49 F4 | U= F0- 2/9 J
F2 10 | Dipole term | F2=F2/49 0.20 | B= F2 -5 F4 0.13 | J = 1/14(F2+F4) 1.15
F4 6.2 | Quadrupole term | F4=F4/441 0.014 | C= 35 F4 0.49 | C = 1/14(9/7F2-5/7 F4) 0.60
Slater & Racah & Kanamori parameters

## Slide 26
3d XAS of rare earths
4f electrons are localized
No effect of surroundings (crystal field < lifetime broadening)
3d XAS is self screened > no charge transfer effect
Initial state
electron-electron interaction.
Valence spin-orbit coupling
Final state
+ core hole – valence hole ‘multiplet’ interaction.
+ core hole spin-orbit coupling

## Slide 27
3d XAS of rare earths
Nd3+ 4f3 system: ground state is 2S+1LJ

## Slide 28
3d XAS of rare earths
Nd3+ 4f3 system: ground state is 4I9/2

## Slide 29
t2g states
Crystal Field Effects
eg states
crystal field effect

## Slide 31
Octahedral crystal field splitting
metal ion
in free space
in symmetrical field
t2g
yz xz xy
eg
in octahedral ligand field
x2-y2 z2
x2-y2 yz z2 xz xy
CRYSTAL FIELD EFFECT
3d1
2D
2Eg
2T2g

## Slide 32
Atomic Multiplet Theory
CRYSTAL FIELD EFFECT
3dN
J=0
J=4
J=1
J=2
J=3
A1
T2
T1
E
A1
E
T2
A2
T2
T1
T1
    Branching rules:
    Same rules for any quantum number
    S, L or J

## Slide 33
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS

## Slide 34
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5

## Slide 35
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5
Dipole selection rule:
ΔJ=T1
(cubic symmetry)

## Slide 36
Comparison with Experiment
2p XAS of ScF3 with crystal field multiplets
PHYS. Rev. B. 41, 928 (1990) [google drive]

## Slide 37
Atomic Multiplet Theory
Crystal Field in square planar symmetry
Approximate CO layer as square planar in symmetry
(Ignore Ni surface)

## Slide 38
Atomic Multiplet Theory
Crystal Field in D4h symmetry
SO3 | Oh | D4h |  | 
S | A1 | A1 |  | 
P | A2 | B1 |  | 
D | E | E |  | 
F | T1 | A2 |  | 
G | T2 | B2 |  | 

## Slide 39
Atomic Multiplet Theory
Simulate angular dependent XAS spectra from the (perpendicular) E
and (parallel) A2 operators
Crystal Field in square planar symmetry

## Slide 40
Atomic Multiplet Theory
Switch off 2p3d interactions (multiplets)
The orbital energy positions (bottom) are different from the spectral peak positions due to the 2p3d electron-electron interactions.
[Difference between DFT and multiplets]

## Slide 41
Charge Transfer Effects
Why different theory in XAS and XPS?
X-ray absorption and x-ray photoemission both involve the same interaction of x-rays with matter.
The theory of XAS and XPS is quite different

## Slide 42

Charge Transfer Effects
3d8
3d9L
9
8
Charge transfer effects in XAS and XPS
Transition metal oxide: Ground state: 3d8 + 3d9L

## Slide 43
3d9L
Transition metal oxide: Ground state: 3d8 + 3d9L

3d8
XPS
2p53d8
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 44
3d9L
Transition metal oxide: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

3d8
2p53d9L
XPS
2p53d8
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 45
3d9L
Transition metal oxide: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 
XAS
2p53d10L
+U-Q  

2p53d9
3d8
2p53d9L
XPS
2p53d8
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 46
XPS:
Screening of the core hole (charge transfer > Anderson impurity model)
+ multiplet effects + crystal field effects
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS
XAS:
Screening of the core hole is small (self screened excitation)
Multiplet effects + crystal field effects (CFM)

## Slide 47
Charge transfer effects in XAS and XPS
When is charge transfer needed in XAS
XAS: Screening of the core hole is small
Charge transfer needed in XAS:
High-valent ions (negative charge transfer)
CO and CN ligands (π-backbonding)
[Metallic & covalent systems]

## Slide 48
=10
NiO
La2Li½Cu½O4
30% 3d8
1A1
30% 3d8
3A2
=-5
=5
=0
=-10
3d8 + 3d9L
Charge Transfer effects
Chem. Phys. Lett. 297, 321 (1998)
Charge transfer effects in XAS

## Slide 49
3d6L
3d5

2p53d7L
2p53d6
+U-Q  
FeIII: Ground state: 3d5 + 3d6L
LMCT and MLCT:  - bonding
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)

## Slide 50
3d4L
3d6L
3d5
FeIII: Ground state: 3d5 + 3d6L + 3d4L

2p53d5L
2p53d7L
2p53d6
+U-Q   - 2

-U+Q   + 2
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 51
FeIII(tacn)2
FeIII(CN)6
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 52
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
(4d, 5d)
4f, 5f
3d ions
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 54
XPS:
Screening of the core hole dominates
Use the 2-state cluster model
Charge transfer effects in XAS and XPS
XAS:
Core hole is screened by excited electron (exciton)
Second state can be ignored
Use the 1-state cluster model
- [a.k.a. the crystal field model]
The 2-state cluster model for core XPS and XAS
[de Groot & Kotani, core level spectroscopy of solids (2008)]

## Slide 55
Model parameters (eg 2-state cluster model):
No direct relation to spectrum
, V(Γ), U, Q, etc.
Spectrum follows from parameters
Charge transfer effects in XAS and XPS
Spectroscopic parameters:
Derived from spectral shape
U, Auger parameter, chemical potential, etc.
Useful to derive relations between both parameter sets
Model parameters & Spectroscopic parameters

## Slide 56
LaF3: La3+ ionic system: Δ = 13 eV
Ground state: 99% pure 4f0, less than 1% 4f1L
Charge transfer effects in XAS and XPS
4f1L
=13 eV
4f0
Ground State
2-state cluster model for 3d XPS of LaF3

## Slide 57
LaF3: La3+ ionic system: Δ = 13 eV
Ground state: 99% pure 4f0, less than 1% 4f1L
Charge transfer effects in XAS and XPS
4f1L
=13 eV
4f0
3d94f1L
XPS
3d94f0
-Q ≈0
Ground State
2-state cluster model for 3d XPS of LaF3

## Slide 58
LaF3: La3+ ionic system: Δ = 13 eV
Ground state: 99% pure 4f0, less than 1% 4f1L
Charge transfer effects in XAS and XPS
3d94f1L
XPS
3d94f0
-Q ≈0
Bonding
combination
Anti-bonding
combination
2-state cluster model for 3d XPS of LaF3

## Slide 59
Charge transfer effects in XAS and XPS
charge transfer
3d spin-orbit
3d4f multiplets
Invisible:
4f spin-orbit ≈ 100 meV
Crystal field ≈ 20 meV
2-state cluster model for 3d XPS of LaF3
[Kotani & Ogasawara, J. Elec. Spec. 60, 257 (1992)]
[Wrongly assigned on
ThermoFischer XPS pages]

## Slide 60
Charge transfer effects in XAS and XPS
Charge transfer?
3d spin-orbit
3d4f multiplets
Invisible:
Crystal field ≈ 20 meV
2-state cluster model for 3d XPS of GdNi
[Chuang et al. PRB 101, 115137 (2020)]
4f spin-orbit

## Slide 61
Gd3+ system: Δ = 15 eV
4f7 has many configurations due to 4f4f interactions
Q < , so -Q >0 and weak mixing
Charge transfer effects in XAS and XPS
4f8L
(eff)=15 eV
4f7
3d94f8L
XPS
3d94f7
-Q > 0
Ground State
2-state cluster model for 3d XPS of Gd systems

## Slide 62
3d10L
Transition metal oxide: Ground state: 3d9 + 3d10L
Energy of 3d9L: Charge transfer energy 
=3
3d9
2p53d10L
XPS
2p53d9
-Q
=-4
Ground State
Charge transfer effects in XAS and XPS
2-state cluster model for 2p XPS of CuBr2

## Slide 63
Charge transfer effects in XAS and XPS
2-state cluster model for 2p XPS of CuBr2
Experiment and calculation from 1981
[van der Laan et al., PRB 23, 4369 (1981)]
charge transfer
2p spin-orbit
2p3d multiplets
3d spin-orbit ≈ 50 meV (invisible)
crystal field ≈ 1 eV (not sensitive)

## Slide 64
Charge transfer effects in XAS and XPS
2-state cluster model for 2p XPS of NiBr2
2-state model can explain 2 features: 3d8 + 3d9L
Need third state for third feature
[Okada et al. J. Elec. Spec. 58, 325 (1992)]

## Slide 65
3d9L
Transition metal oxide: Ground state: 3d8 + 3d9L + 3d10L2
Energy of 3d9L: Charge transfer energy 
Energy of 3d10L2 : 2 + U (due to extra 3d3d interaction)
=0.5
3d8
Charge transfer effects in XAS and XPS
The 3-state cluster model for core XPS
3d10L2
2+U = 7.5

## Slide 66
3d9L
=0.5
3d8
Charge transfer effects in XAS and XPS
The 3-state cluster model for core XPS
3d10L2
2+U = 7.5
2p53d9L
2p53d10L2
2p53d8
-Q = -7.0
2+U-2Q
=-7.5
[Okada et al. J. Elec. Spec. 58, 325 (1992)]

## Slide 67
What is the value of U (NiO)
(ZSA) LDA GGA meta-GGA (SCAN) 1985
UZSA = 6
UDFT =U ZSA
time

## Slide 68
What is the value of U (NiO)
(ZSA) LDA GGA meta-GGA (SCAN) 1985
UZSA = 6
UDFT =U ZSA
time
Self-consistent UDFT
UDFT = ~ 0

## Slide 69
What is the value of U (of NiO)
(ZSA) LDA GGA meta-GGA (SCAN) 1985
{XAS, XPS, AES, RPES, RIXS}
UZSA = 6 UZSA = 6
UDFT =U ZSA
time
Self-consistent UDFT
UDFT = ~ 0

## Slide 70
Charge transfer effects in XAS and XPS
3-state cluster model for 2p XPS of NiO
3-state model does not explain feature at 855 eV
New screening channel: non-local screening
Electron hops from neighboring metal ion to metal ion with core hole
All channels can be included by coupling to density-of-states (DOS)
DOS calculated by Dynamical Mean Field Theory (DMFT)
3-state model
DMFT + multiplets
Experiment
[Ghiasi et al., PRB 100, 075146 (2019)]

## Slide 71
1s XPS spectra
charge transfer
multiplet effects (2p3d)
non-local screening
[Ghiasi et al., PRB 100, 075146 (2019)]

## Slide 72
[Ghiasi et al., PRB 100, 075146 (2019)]
1s XPS spectrum has multiple peaks
One photon energy relates to many different electron kinetic energies:
>>> K edge XAS is influenced by photo-excitation
>>> Kα XES is influenced by photo-excitation
1s XPS spectra

## Slide 73
atomic
multiplet
theory
(DFT)
BSE GW+C
Interpretation of core XPS (XAS)
Intra-atomic e-e interactions
Interatomic interactions (mean field)
crystal field
multiplet
theory
charge fluctuations
(Δ, U, Q)
impurity
multiplet
theory
DMFT+
multiplets
4f ionic 3d covalent 3d (f) no open l d or f
X
X
X
The d and f states react much stronger to core holes >> This is true for oxides and also for metals