## Slide 1
Introduction to XAS
Overview of x-ray and electron spectroscopies
Interpretation of XAS
XAS experiments
  Transmission
  Electron Yield
  Fluorescence Yield
X-ray Absorption Spectroscopy

## Slide 2
X-ray sources

## Slide 3
X-ray monochromator
x-ray monochromator

## Slide 4
X-ray Absorption Spectroscopy
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 5
X-ray spectroscopies
3d8 + ω

## Slide 6
3d8 + ω
2p53d9
X-ray spectroscopies
XAS

## Slide 7
3d8 + ω
2p53d9
2p53d8+e’
XPS
X-ray spectroscopies
XAS

## Slide 8
X-ray absorption
XAS: decay of the core hole
core holes live only a few femtoseconds
Notes: 8

## Slide 9
X-ray emission
XAS: decay of the core hole: x-ray emission
Notes: 9

## Slide 10
Auger
XAS: decay of the core hole: Auger
Notes: 10

## Slide 11
XAS: decay of the core hole: Auger and XES
Below 1000 eV: 99% Auger decay

## Slide 12
Electron escape depth
Electron yield has few nm probing depth

## Slide 13
3d8 + ω
2p53d9
2p53d8+e’
XPS
X-ray spectroscopies
XAS

## Slide 14
3d8 + ω
2p53d9
2p53d8+e’
XPS
3p43d9+e’
RXES (RIXS)
3d8 + ω’
RAES
XES
3d7 +e’+ω’
X-ray spectroscopies
IXS
3p43d8 +e’+e ’’
AES
XAS
XES
AES
AES
XES

## Slide 15
3d8 + ω
2p53d9
2p53d8+e’
XPS
3p43d9+e’
RIXS
3d8 + ω’
RAES
XES
3d7 +e’+ω’
X-ray spectroscopies
IXS
3p43d8 +e’+e ’’
AES
XAS
Negative -1 -2
XES
AES
AES
XES

## Slide 16
Neutral experiments are self-screened
XAS, RIXS, (optical, EPR)
>> small screening satellites
>> crystal field theory can be used
Ionising experiments are not self-screened
XPS, RAES
>> large screening > large satellites
>> crystal field theory can not be used
Charge Transfer Effects
Neutral experiments

## Slide 17
3d8 + e
Electron spectroscopies 1

## Slide 18
3d8 + e
2p53d9 +e’
2p53d8+e’
cEELS
Electron spectroscopies 1
cEELS

## Slide 19
3d8 + e
2p53d9
+e’
2p53d8+e’
cEELS
3p43d9+e’
3d8 + ω’
XES (EDX)
3d7 +e’+ω’
Electron spectroscopies 1
3p43d8 +e’+e ’’
AES
cEELS
XES
AES
AES
XES

## Slide 20
3d8 + e
2p53d9
+e’
2p53d8+e’
cEELS
XES (EDX)
3d7 +e’+ω’
Electron spectroscopies 1
3p43d8 +e’+e ’’
AES
cEELS
negative
AES
XES
all excitations at once,
no resonant experiments

## Slide 21
3d8 + e
2p53d10
Electron spectroscopies 2
XES
RIPES
3d9 + ω’
3d8+e’
AES
REELS
EELS
EAS (APS)
positive

## Slide 22
Neutral experiments are self-screened
XAS, RIXS, (optical, EPR), EELS
>> small screening satellites
>> crystal field theory can be used
Ionising experiments are not self-screened
(R)XPS, (R)Auger. (R)IPES, APS
>> large screening > large satellites
>> crystal field theory can not be used
Charge Transfer Effects
Neutral experiments

## Slide 23
3d8 + ω
2p53d9
2p53d8+e’
XPS
3p43d9+e’
RIXS
3d8 + ω’
RAES
XES
3d7 +e’+ω’
X-ray spectroscopies
IXS
3p43d8 +e’+e ’’
AES
XAS
XES
AES
AES
XES

## Slide 24
3d8 + ω
2p53d9
X-ray spectroscopies
XAS

## Slide 25
Element specific
Sensitive to low concentrations
Applicable under extreme conditions
SPACE: x-ray spectromicroscopy
TIME: femtosecond XAS
RESONANCE: RIXS, RAES
+ scattering, +reflectivity
X-ray Absorption Spectroscopy
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 26
Label
Orbital
eV
K
1s
6539
L I
2s
769
L II
2p1/2
650
L III
2p3/2
639
M I
3s
82
M II
3p1/2
47
M III
3p3/2
47
X-ray absorption edges
X-ray Absorption Spectroscopy
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."
sharp
principal
diffuse
fundamental
J. Chem. Educ. 84, 757 (2007)

## Slide 27
X-ray Absorption Spectroscopy
Atomic electronic structure X-ray absorption of an oxygen atom
(Rydberg states)

## Slide 28
XAS of oxygen ions
ion electrons binding energy (eV)
O 8 528.8
O1+ 7 533.3
O2+ 6 537.2
O3+ 5 545.8
O4+ 4 554.6
O5+ 3 562.3
Higher binding energy indicates a higher valence

## Slide 29
X-ray Absorption Spectroscopy
Molecular electronic structure X-ray absorption of an O2 molecule
(σ* mixed with Rydberg states)

## Slide 30
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
XAS: spectral shape (O 1s)
Electronic structure of a transition metal oxide
Main bonding:
O2p with metal 4sp
Gives valence band and conduction band,
Mixed in character
Additional bonding
O2p with metal 3d;
Gives mixed 3d bands split by crystal field in octahedral symmetry, T2g states have pi-bonding and Eg states have sigma-bonding.
oxygen 1s core state
is localized at an oxygen atom
Notes: 30

## Slide 31
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
XAS: spectral shape (O 1s)
transition from oxygen 1s state
to an empty state
oxygen 1s core state
is localized at an oxygen atom
local empty DOS
dipole selection rule:
p-projected DOS
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
[Phys. Rev. B. 40, 5715 (1989); review in Chem. Rev. 120, 4056 (2020)]
Notes: 31

## Slide 32
Final State Rule: Spectral shape of XAS looks like final state DOS
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape

## Slide 33
Ground state
Occupied O 2p valence band
Empty Ti 3d conduction band
Crystal field split 3d band
O 2p
valence
band
Eg
T2g
Oxygen 1s XAS
O 2p states more localized
Reduced bonding
Reduced crystal field
The crystal field splitting is reduced in the oxygen K edge
XAS: Final State Rule

## Slide 34
Ground state
Occupied O 2p valence band
Empty Ti 3d conduction band
Crystal field split 3d band
O 2p
valence
band
Eg
T2g
Oxygen 1s XAS
O 2p states more localized
Reduced bonding
Reduced crystal field
Titanium 2p XAS
Ti 3d states more localized
Reduced bonding
Reduced crystal field
The crystal field splitting is reduced in the oxygen 1s XAS and also in metal 2p XAS
XAS: Final State Rule
XAS crystal field is smaller than the optical crystal field
(& the DFT ground state crystal field)

## Slide 35
XAS: spectral shape (O 1s)
Crystal structure
Electronic structure calculation, for example Density Functional Theory (DFT)
(in the presence of the core hole)
Calculation of the oxygen
p-projected local empty DOS
Compare with experiment
CODES: FEFF, Wien2K, VASP, QE, etc.

## Slide 36
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect the d (and s-) projected Ti DOS
Why is experiment different?
2p > 3d
Notes: 36

## Slide 37
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect the d (and s-) projected Ti DOS
2p spin-orbit coupling (~6 eV)
2p > 3d
Notes: 37

## Slide 38
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect local d-projected Ti DOS
Core spin-orbit splitting
Overlap of core 2p and valence 3d states
>> many electron excitations dominate
2p3d 2-electron integrals
Notes: 38

## Slide 39
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
IXAS = |< 2p5 3d1 |dipole| 3d0>|2 [E=0]
Single electron (excitation) approximation breaks down :
IXAS = |<3d |dipole| 2p>|2 
X-ray absorption
XAS: spectral shape (Ti 2p)
Can NOT approximate 2p-3d interaction as extra potential
Large core hole spin-orbit coupling

## Slide 40
2p3/2
2p1/2
Core-valence electron-electron interactions NOT screened in solids
Single Particle (excitation) models break down [both DFT & BSE]
3d
<2p3d|1/r|2p3d>
XAS: multiplet effects
[Phys. Rev. B. 42, 5459 (1990)]

## Slide 41
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
IXAS = |< 1s1 2p5 |dipole| 2p4>|2 [E=0]
Single electron (excitation) approximation :
IXAS = |<2p |dipole| 1s>|2 
X-ray absorption
XAS: spectral shape (O 1s)
Can neglect local 2p-2p interaction
Can approximate 1s-2p interaction as extra potential
No core hole spin-orbit coupling

## Slide 42
atomic
multiplet
theory
(DFT)
TD-DFT
BSE
Interpretation of XAS
Intra-atomic e-e interactions
Interatomic interactions (mean field)
crystal field
multiplet
theory
Strong correlations
impurity
multiplet
theory
(GW+C)?
DMFT+
multiplets
4f ionic 3d covalent 3d (f) closed shell

## Slide 43
TD-DFT
BSE
Interpretation of XAS
1-particle excitation (electron – core hole)
Neglect many-electron interactions
3d3d multiplets
2p3d multiplets
Ligand-metal charge transfer (Δ)
Metal-metal charge transfer (U)
Two core holes

## Slide 44
Experiments
X-ray Absorption Spectroscopy

## Slide 45
XAS in transmission: STXM example
Nanoscale chemical imaging of a working catalyst

## Slide 46
Carbon K-edge
[de Smit, Nature 456, 222 (2008)]
XAS in transmission: STXM example
Nanoscale chemical imaging of a working catalyst

## Slide 47
X-ray enters sample
Total absorption
Penetration depth λ is inverse proportional to
Yield detection
λ
XAS measured with total electron yield

## Slide 48
Core hole decays by x-ray
photons (σX) or electrons (σE)
Electrons escape from surface determined by their kinetic energy λ
Electron yield: EY = * σE * λ ~
[Neglect angular dependences]
Electron Yield detection
λ
λ
XAS measured with total electron yield

## Slide 49
XAS with TEY: electron escape depth
vacuum Dy Ni
Electron escape depth (TEY):
Detect Ni 2p XAS as function of Dy layer thickness: Intensity can be simulated with escape depth d = 1,1 nm
X-rays
[Vogel, J Elec Spec 67, 181 (1994)]

## Slide 50
Partial and conversion EY:
Partial Electron yield:
Detect kinetic energy of electrons:
Select specific photoemission or Auger yield
(position of detector to study angular effects)
Conversion Electron Yield (in gas environment):
Electrons ionize gas ions
> Separate signal from direct x-ray ionization of gas > Determine linearity between intensity and ionization
> Avoid (indirect FY effects)

## Slide 51
Core hole decays by photons (σ) or electrons (σE)
Photons escape prop. to λ
Fluorescence yield: FY = * σ * λ
[Neglect angular dependences]
Fluorescence Yield detection
λ

## Slide 52
Fluorescence yield: FY = * σ * λ
= +
λ ~1/
σ is different for edge and background (σB)
Fluorescence Yield detection
ITFY ~

## Slide 53
FY detection: dilute sample
ITFY ~
Non-d
ITFY ~
ITFY ~

## Slide 54
Single synchrotron pulselength is too long
FY detection: state dependent decay
Mitzner, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 54

## Slide 55
Fluorescence does not measure XAS spectrum
Saturation ?
FY detection: state dependent decay
Mitzner, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 55

## Slide 56
Fluorescence does not measure XAS spectrum
NO Saturation
State-dependent decay
Mitzner, J. Phys. Chem. Lett. 4, 3641 (2013)
FY detection: state dependent decay
Notes: 56

## Slide 57
Yield methods assume a constant ratio between radiative and non-radiative decay
If this ratio is state (= energy) dependent than the related yield methods do not measure XAS.
The dominant yield method is not visibly affected, thus for soft X-rays only FY is affected, not electron yield.
FY detection: state dependent decay

## Slide 58
FY*500
EY
L3
L2
Solid State Comm. 92, 991 (1994)
FY detection: state dependent decay

## Slide 59
FY detection (state-dependent, dilute)
ITFY ~
ITFY ~
Main decay of 2p core hole is 2p3d RIXS
Integrate RIXS spectrum to 2p3d PFY
TFY ~ 2p3d PFY
NOTE: “RIXS” has angular dependence effects

## Slide 60
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
FY detection: state dependent decay
Notes: 60

## Slide 61
ITFY ~ = the integrated RIXS
Measure the partial fluorescence yield of the background.
IBFY ~
1/(1+x) ≈ 1 – x
IBFY ≈ 1 –
Measure a negative XAS spectrum, essentially tracking the probing depth [λ]
Inverse PFY
Achkar, scientific reports 1, 82 (2011)

## Slide 62
Achkar, scientific reports 1, 82 (2011)
Inverse PFY

## Slide 63
FY detection: dips and peaks
Measure the total fluorescence yield
Positive (saturated) state-dependent metal PFY
+ Negative inverse oxygen PFY
ITFY ~
ITFY ~ c1

## Slide 64
FY detection: dips and peaks
Nature Chem. 4, 766 (2012) & Phys. Rev. Letter discussions (2014)

## Slide 65
Different PFY signals
Chiu, Nature Rep. 11, 5250 (2021)
IPFY: small signal, no saturation
2p3s PFY: minor saturation, large sCK effect
2p3d PFY: large saturation, state-dependent decay

## Slide 66
Different PFY signals
PFY/RIXS:
10 meV: Few RIXS beamlines; small signal, conceptually possible to measure XAS with 10 meV resolution (put detector at sharp peak)
100 meV: Most RIXS beamlines
1 eV: TES detector
10 eV: Dedicated fluorescence detectors
100 eV: Fluorescence detectors
Inverse relation between resolution and intensity

## Slide 67
Transmission
(pinhole, saturation > thin samples)
Electron Yield
(surface sensitive)
Fluorescence Yield
(saturation & self-absorption:
> dilute samples)
[L edges are intrinsically distorted]
XAS: detection techniques