## Slide 1
Crispy: A Graphical User Interface for X-Ray Spectroscopy Calculations
Marius Retegan
Algorithms & scientific Data Analysis (ADA) Group

## Slide 2: Semi-Empirical MultipletS: the early days
B.T. Thole et al.,
Phys. Rev. B, 1985, 35, 6856
F.M.F. de Groot et al.,
Phys. Rev. B, 1990, 42, 5459
Notes: - In the early days
- The ground state of the diluted manganese in silver is d5

## Slide 3: Quanty: a modern approach to multiplets calculations

## Slide 4: Crispy: A user interface for Semi-empirical multiplets
https://silx.org
Read/write tools for various data formats
Data reduction routines
A set of Qt widgets to browse and visualize the data

## Slide 5: Getting the software
https://crispy.esrf.fr
crispy + esrf

## Slide 6: Supported Systems
3d
Sc – Cu
XAS / XPS: K, L1, L2,3, M1, M2,3 · XES: Kα, Kβ
RIXS: K-L2,3, K-M2,3, L2,3-M4,5
Y – Ag
XAS / XPS: L1, L2,3, M1, M2,3, M4,5, N1, N2,3
RIXS: L2,3-N4,5
Hf – Au
XAS / XPS: L2,3, M2,3, M4,5, N2,3, N4,5, O2,3
RIXS: L2,3-O4,5
La – Yb
XAS / XPS: L2,3, M2,3, M4,5, N2,3, N4,5
RIXS: L2,3-M4,5, L2,3-N4,5, M4,5-N6,7
Ac – Cf
XAS / XPS: L2,3, M2,3, M4,5, N2,3, N4,5
RIXS: L2,3-M4,5, L2,3-N4,5, M4,5-O6,7
3d
4d
5d
4f
5f
Oh
Td
D4h
D3h
D3d
C3v

## Slide 7: Hamiltonians
S. M. Butorin et al., Chemistry - A European Journal, 2016, 22 (28), 9693–9698
 | Atomic | Crystal Field | Ligand Field
Time (s) | 0.5 | 0.5 | 126
Atomic
Crystal Field
Ligand Field
Atomic
Crystal Field
Ligand Field

## Slide 8: Special Hamiltonian Terms
V. Vercamer et al., Phys. Rev. B, 2016, 94, 245115

## Slide 9: Orientation-Averaged RIXS
S. Zhang, O. Bunău et al., accepted to Phys. Rev. B
current
previous

## Slide 10: Loading and Saving Data
A dedicated widget allows to open ASCII data files.
The results can be serialized and deserialized to a HDF5 file format, that can be be visualized with utils like silx view.

## Slide 11: Parameter Scan: Integrated Widget and Jupyter Notebooks
Widget
Jupyter Notebook

## Slide 12: Application of the XMCD sum-rules

## Slide 13: XMCD Sum rules for L2,3 edges
Jafri et al., Inorg. Chem., 2016

## Slide 14: The magneto-optical sum rules

## Slide 15: Sum rules in practice
The sum rules can provide very useful information on the magnetic electronic
structure by separating the orbit and spin parts of the magnetization.
Origin of problems in the application of the sum rules:
  Removal of the transitions towards continuum states is done by subtracting parameterized arctangent functions.
  The cutoff energy between L3 and L2 edges in the XMCD spectrum.
  Intermixing of L3 and L2.

## Slide 16: Experimental data
Experimental details:
  the metal atom in FeTp is Fe3+
  temperature (T = 2 K)
  magnetic field (B = 6.5 T)
Measured spectra: http://bit.ly/multiplets

## Slide 17: Calculations using octahedral (Oh) symmetry
 | ⟨Sz⟩ | ⟨Lz⟩ | ⟨Tz⟩
Jafri et al. | −0.1786 | −0.8521 | −0.0523
Calculate the spectrum using the following parameters:
    Lorentzian FWHM: 0.5
    Gaussian FWHM: 0.24
    scale factors: Fk = Gk = 0.7, zeta = 1.0
After the first calculation, open the “Details” dialog and normalize the spectrum to the maximum.
Increase the 10Dq value in steps of 0.5. Note the effect on the calculated spectrum. Are any features that start appearing in the spectrum for larger 10Dq? Follow the changes in the expectation value of the ⟨Sz⟩ operator.
Note the expectation values of the spin (S), orbital (L), and magnetic dipole (T) operators for 10Dq = 2.8 eV. How do they compare with the calculations from the original publication?

## Slide 18: Ligand field calculation in octahedral symmetry
 | ⟨Sz⟩ | ⟨Lz⟩ | ⟨Tz⟩
Jafri et al. | −0.1704 | −0.7754 | −0.0594
Hocking et al., J. Am. Chem. Soc., 2006
Note the additional features appearing in the spectrum and the changes in the expectation values; compare them with the ones from the original publication.
Add the metal-ligand hybridization charge transfer (MLCT) term with the following parameters:
Δi = 3.0, Δf = 3.4, V(eg) = −0.8, V(t2g) = 1.8.

## Slide 19: In search of the missing peak
Change the symmetry to C3v and rerun the calculation using the following parameters for the crystal field:
  Dq = 0.28 eV (≡ 10Dq = 2.8 eV)
  Dσ = 0.07 eV
  Dτ = 0.12 eV
Did you manage to reproduce the feature f?
t2g
eg
e
a1
e

## Slide 20: Utility of multiplets calculations
What is the value of ⟨Tz⟩?
Test the validity of the sum rules and determine the origin of their potential failures.

## Slide 21: Crystal field and covalency effects in uranates

## Slide 22: Crystal field and covalency effects in uranates

## Slide 23: Crystal field and covalency effects in uranates
1) Calculate the atomic M4 spectrum for U5+ using the following parameters:
  scale factors: Fk = Gk = 0.7
  Lorentzian FWHM: 0.35 eV
  Gaussian FWHM: 0.8 eV
2) Add a crystal field contribution with Wybourne’s parameters:
  B40 = 2.03 eV
  B60 = 0.17 eV
3) Finally, add the hybridization term with the ligands (LMCT):
  Δ = 4.0 eV,
  U(5f,5f) = 3.5 eV
  U(3d,5f) = 6.0 eV
  Vi = 1.2 eV, and Vf = 0.9 eV

## Slide 24: Calculating the L2,3–edge XAS spectrum of titanium(IV)

## Slide 25: Theory and calculations
de Groot et al., J. Chem. Minerals, 1992

## Slide 26: Atomic multiplets
Calculate the XAS spectrum at the L2,3 edges of Ti4+ in spherical symmetry. Set the Lorentzian broadening to 0.1 and the Gaussian broadening to 0.0. Leave all the other parameters to their default values. How many transitions are visible in the spectrum?
Run a calculation with the scaling of the 2p spin-orbit coupling constant, ζ(2p), set to 0.5. After the calculation finishes, set this value back to 1.0 and run a second calculation with the 3d spin-orbit coupling ζ(3d) set to 0.5. Which interaction affects the most the energy separation between the L2 and L3 edges? Check that the energy separation between the two edges is close to 3/2·ζ(2p).
Perform three calculations using 0.8, 0.4, and 0.0 for scaling the Slater integrals, Fk and Gk. What is the influence of electronic repulsions on the spectrum?

## Slide 27: Crystal-field multiplets
Set the scaling factors for the Slater integrals back to 0.8. Re-enable the crystal field and change the 10Dq value to 2.0 eV.
Change the Lorentzian broadening to 0.2, 0.4, 460. This will apply a 0.2 eV broadening at the L3 edge and a 0.4 eV at the L2 edge and will change between the two broadenings at 460 eV.
Run a set of calculations with 10Dq ranging from 0 to 2.0 eV in steps of 0.5 eV. Plot the resulting spectra. What is the influence of the crystal field splitting?
Set the 10Dq value to 2.0 eV and switch off the Slater integrals and the 3d spin-orbit coupling. How many transitions does the calculated spectrum have?

## Slide 28: Following spin transitions in iron compounds

## Slide 29: Using K pre-edge XAS to identify spin states
Write down the electronic configuration of Fe3+. Show that there are two ways to fill the 3d orbitals, leading to a high spin (S = 5/2) and a low spin ground state (S = 1/2).
Run two K pre-edge calculations for Fe3+ in an octahedral crystal field, one with 10Dq set to 2.0 eV and 3.3 eV.
Change the 10Dq value from 2.6 to 3.6 eV in steps of 0.2 eV. At what value do you observe the spin transition?
Westre et al., J. Am. Chem. Soc., 1997